**3**



Data Analysis of Tata Steel Sinter Plant using Auto ML

BATCH HOT DIP GALVANZING OF STEEL

**Name of Student :** Krishna Deshpande

**Name of College :** Vellore Institute of Technology, Chennai Campus

**Internship Done at :** Tata Steel Limited

**Duration :** 10 weeks (04/09/2023 to 14/11/2023)

**Subject :** Data Analysis of Sinter Plant using Auto ML

**Name of Guide :** Mr. Nitish Kumar (Head Analyst, Tata Steel)

**Name of Sponsor :** Mr. R. Krishna (Chief Analytics Officer, Tata Steel)

**Abstract**

Integrated steel making process involves production of steel right from using iron ore from mines to the finished steel product. The production process goes through different processing stages and at each stage, process must achieve its desired output to meet the next process requirement. All these processes are interlinked and therefore deviation in any one process can lead to the deterioration in product quality or productivity in the next process.

Sintering is one of the key processes in Integrated Steel Plant. In Sintering process, iron ore fines are agglomerated with coke on a moving conveyer bed. This happens at the temperature of around 1350 - 1400 Deg C. There are multiple variables such as Temperature, Speed of the Conveyer, Ratio of Iron Ore fine vs Coke, etc which determines final Sinter quality. In this project, a correlation between various process parameters is developed by using different Machine Learning Tools so that the outcome can be used to effectively to control the sinter process to get the best product quality and productivity.

**Contents**

[1. Introduction 5](#_Toc53839078)

[2. Integrated Steel Plant Production Process 5](#_Toc53839079)

[2.1 Product Process Overview 5](#_Toc53839080)

[2.2 Iron Making 6](#_Toc53839081)

[2.3 Steel Making 7](#_Toc53839082)

[2.4 Steel Products 7](#_Toc53839083)

[3. Why Sintering 8](#_Toc53839086)

[4. Sintering Process 9](#_Toc53839087)

[5. Process Variable & Data Capatuing 11](#_Toc53839093)

[5.1 Conveyor 11](#_Toc53839094)

[5.2 Mixing Drums 11](#_Toc53839095)

[5.3 Sinter Breaker 11](#_Toc53839096)

[5.4 Exhauster 11](#_Toc53839097)

[5.5 Speed 11](#_Toc53839098)

[5.6 Size 12](#_Toc53839099)

[5.7 Temperature 12](#_Toc53839100)

[6. Deliverable of the Project 13](#_Toc53839101)

[7. Steps Taken 14](#_Toc53839108)

[7.1 Exploring the data 14](#_Toc53839109)

[7.2 Preprocessing of the data 14](#_Toc53839110)

[7.3 Cleaning the data 15](#_Toc53839111)

[7.4 Data Modelling 18](#_Toc53839112)

[7.5 Model Optimization 18](#_Toc53839113)

[8. Selection of Machine Learning Tools 19](#_Toc53839114)

[8.1 Linear Regression 19](#_Toc53839115)

[8.2 Random Forest Regression 19](#_Toc53839116)

[8.3 Support Vector Regression (SVR) 20](#_Toc53839117)

8.4 Ridge Regression …………………………………………………………………………………………………………………..20

8.5 Lasso Regression …………………………………………………………………………………………………………………..20

8.6 Least Angle Regression (LARS) .……………………………………………………………………………………………..21

8.7 Gradient Boosting Regression .………………………………………………………………………………………………21

8.8 XGBoost Regression ………………………………………………………………………………………………………………22

8.9 Elastic Net Regression …………………………..………………………………………………………………………………22

8.10 Bayesian Ridge Regression …………………………………….……………………………………………………………22

8.11 Kernel Ridge Regression ………………………..……………………………………………………………………………23

8.12 Stochastic Gradient Descent (SGD) Regression …………………………………………………………………..23

8.13 Decision Tree Regression ………………………….……………..…………………………………………………………24

8.14 adaboost Regression ……………………………….….………………………………………………………………………24

8.15 Table showing the differential characteristics of each model ……………………………………………..25

[9. Best Suitable ML Tool](#_Toc53839118) 26

[10. Conclusion](#_Toc53839125) 26

[11. References](#_Toc53839126) 27

[12. Acknowledgment](#_Toc53839127) 27

# Introduction

India is blessed with Iron Ore mines. Majority of these mines are located towards the eastern part of the country. Tata Steel (Earlier name TISCO – Tata Iron & Steel Company) is the first Indian company who started production of steel way back in 1914 at Jamshedpur. For production of steel, Iron Ore, Coke, and Limestone are required as a raw material, which are abundantly available in the eastern belt of India.


As a part of Integrated Steel making process, Iron ore & Coke are fed to the Blast Furnace to get the liquid iron. However, iron ore fines cannot be used in blast furnace. Hence, they are agglomerated through a process called Sintering. The Sintering process is bit complex, which involves multiple variable such as Temperature, Conveyer Speed, etc.

In the past, Steel Industries were operating this process in a crude way. Capturing the process information has always been a challenge due to difficult operating environment such iron fine dust, high temperature, etc. Therefore, control over the final product quality was not precise. That also led to the issues related productivity and frequent break down. Achieving the right quality and right quantity of Sinter product is most important as it is a part of supply chain to the next process, which is Blast Furnace. Over a period, systems were developed to measure the various process parameters. Now the data was available, however there was a challenge to analyse this big data set. Machine Learning have different tools to analyse various types of data. In this project, we will talk about usage of various Machine Learning Tools for the Data Analysis to get the effective conclusion.

# Integrated Steel Plant Production Process

## 2.1 Production Process

Integrated Steel Plant Production Processes involves getting raw material from mines, processing it and converting it in crude liquid iron and further refining it into the steel at steel making stage. The liquid steel is then casted to convert it into the solid slab which is then rolled into Rebar, Wire Rods or Flat Products such as Hot Rolled or Cold Rolled Products.



## *Figure: 1*


## 2.2 Iron Making

Iron Ore, Sinter and Coke are fed via conveyer belt to the Blast Furnace from the top as schematically shown in Figure 2. Hot Air Blast given through the tuyere located at the bottom. This hot air ignites coke, which raises the temperature inside the blast furnace to melt the iron ore, which is taken out from a Tap hole located at the bottom of the Blast Furnace. It is important to maintain adequate proportion of incoming raw material from top, their desired distribution inside the blast furnace to get the best productivity and quality of crude liquid iron.

## *Figure: 2*

## 2.3 Steel making

Crude liquid iron is the input material for Steel making. Steel making is nothing but removing the unwanted impurity from crude liquid iron received from Blast Furnace by process like Desulphurization, Oxidation at Basic Oxidation Furnace (LD Converter) and alloying it to convert it into the required grade of steel. The liquid steel is then converted to sold Billet or Slab by a process known as Casting. There are multiple process involved in steelmaking which are explained in schematic Figure 3.



## *Figure: 3*


### 2.4 Steel Products

Steel Slabs or Billets are then rolled into the final shapes such as Hot Rolled Products or Rebars. Hot Rolled Coils are further rolled into Cold Rolled & Coated Products which are used in Automotive, Furniture and General Engineering Purpose, whereas Rebars are used in Construction Segment.

## *Figure: 4*

# Why Sintering

Iron ore is one of the key raw materials required at Blast Furnace. However, this ore must be in the range of 8 to 30 mm diameter, which gives optimum processing conditions inside the blast furnace. In the Blast Furnace, hot air is blown from bottom, whereas Iron Ore and Coke is charged from the top. This charge gradually moves down, whereas hot air from bottom moves up. The moving hot air helps in burning the coke, which generates heat required for melting of iron ore. For the hot air movement through the charge, there must be some gap between the individual iron ore charge. If the Iron ore is too fine, then there will not be adequate gap for the gases to move up and the fines will choke the furnace. Also, if the iron ore lumps are tool large, it would be difficult for them to melt. This schematically shown in Figure 5. Hence iron ores must be certain size range to get the best outcome.

Iron ore is produced from iron ore mines, but while mining, lot of iron ore fines are generated, which are to the tune of 20 – 30 %. However, these are not suitable for Blast Furnace. To avoid the wastage, it was important to develop a process which will make them suitable for Blast Furnace. Therefore, a process called Sintering is developed in which iron ore fines are agglomerated and converted into lump sizes suitable for Blast Furnace. Sintering has helped in saving the wastage of Iron ore fines, generated at Iron ore mines. 

*Figure: 5*

# Sintering Process

Sintering process is developed mainly to utilize under size of lump ore called iron ore fines; which

otherwise, could not be charged directly in blast furnace. In order to conserve these, otherwise waste material, they are compacted together and made into lumps by a process known as sintering. Sintering is defined as the agglomeration of the Iron ore fines (generally <8 mm) by incipient fusion of fine mineral particles with heat produced by burning of coke breeze, uniformly distributed in raw mix bed. During the sintering process, iron ore fine particles agglomerate into a porous compact heterogeneous lumpy mass called SINTER by incipient fusion caused by the heat produced during the combustion of the solid fuel within the moving bed of loosely particles.

The coke at the top of the blend is ignited by gas burners, that can be fuelled by coke oven gas, blast furnace gas, or natural gas. As the sinter bed moves, air is sucked from the top through the mixture, enabling combustion through the entire layer and complete sintering – where the temperatures may reach 1300 – 1480oC. At the end of the strand, the material is cooled by air and finished sinter is size-screened.

As per given burden, raw materials are collected on a common conveyor from the respective bunkers through weigh feeders and then mixed homogeneously in mixing drums (primary & secondary mixing drums) by adding required water (7 to 8 %) and then feed on sinter machine. Generally, raw mix bed height is 550 mm and is adjusted based on quality of the raw material. The bed in running (motion) condition is taken to ignition front. The raw mix undergoes through the ignition furnace and there is a negative suction from bottom. As soon as suction takes place, hot products of combustion are sucked through the bed and transfer its heat to the next layer of the bed keeping it ready for the combustion. These flue gases are let out from chimney through ESP. After completion of the sintering process, sinter cake will be crushed and screened after discharge from the machine. Sinter having size > 5 mm will go to the cooler and then it will go to BF. Sinter with size < 5 mm size fines will be re-cycled in the process.



*Figure: 6*

# Process Variables and Data Capturing

## 5.1 Conveyors

The conveyor takes the hot mixture of coke and iron ore filings till it reaches the Sinter Breaker. The conveyor is made of a strong metal which doesn’t melt on such high temperatures.



## 5.2 Mixing Drums

These drums carry the iron ore, coke and limestone and put the mixture onto the conveyor. The mixture is very important to be correct as the mixture must agglomerate properly for the iron ore to melt nicely in the blast furnace.

## 5.3 Sinter Breaker

The sinter breaker is a fundamental step in this process as well. This tool is used to make the sinter into relevant sized pieces for the blast furnace. It breaks the newly formed hot sinters into right measures.

## 5.4 Exhauster

The exhausters here are places below the conveyor. These exhausters are used to keep the mixture hot and make them agglomerate evenly from top to bottom.

## 5.5 Speed

The speed of the all the things is linked to the making sinters. The more the speed, the lesser the mixture will get time to agglomerate. If this is not done properly then the sinter would not form correctly. The speed and amount of the iron ore, coke and lime being poured into the conveyor has to be measured in real time to reduce errors. The speed of the conveyor belt also shouldn’t exceed its limits. The mixture usually takes around 30min – 40min to agglomerate into sinters. If the conveyor is sped up, this mixture would still be too hot for the next procedure and would result in bad sinters being thrown into the hot blast furnace.

## 5.6 Size

The size of the sinter should be a minimum of 8mm. All the iron ore filings which go into the sinter plant are below the size of 8mm and they come out bigger than the original so that they could be converted into molten liquid iron in the blast furnace.



## 5.7 Temperature

Temperature is the most critical aspect of the whole process. At the start, when we introduce the iron filings to the conveyor belt, they are at room temperature. Then we have to heat the mixture just enough to make them a bit porous and agglomerate neatly so that they become sinters. The temperature on the conveyor stays between 1300 – 1480 deg C. If this temperature varies, the process will not fruit success. Higher temperature can result in melting and lower temperatures could result in the mixture not agglomerating, keeping them as filings till the end. We also have to make sure this temperature goes through the whole mixture. This is important so that no iron filings go waste.

# Deliverable of the Project

Sintering Plant produces a lot of data. This large amount of data had to be analysed in a structured manner. By analysing the data and making it more structured than before, the data taken from the plant will be more useful for research purposes for the plant.

By using different Data Analysis techniques and Machine Learning models, I had to analyse the Sinter Plant data given to me and make it more relevant for the industry for further conquests.

Making use of techniques like Feature Selection to analyse the data was one of the major tasks. Identifying which data is of what nature was a very needed experience which helped me gain knowledge in doing data analysis.

# Steps taken

## 7.1 Exploring the Data

The first task of Data Analysis is exploring the data and taking note of what all data is given. I had been given 5000 entries and 14 different columns of data denoting different aspects of the sintering process.


We first check if we had any null values in the data set provided. The elimination or filling the gaps of errors like null variables give us better results while using ML tools for good results. When we checked we got no null values, which was a very good result for us.

‘CLOCK’ and ‘OUTPUT’ were 2 columns of data which were labelled while others were named from X1 till X14. The datatype of ‘CLOCK’ column was ‘object’ type, which was not useful for us while doing data analysis.

## 7.2 Preprocessing of the Data

Making sure all the data are of relevant datatypes and none of the data has loopholes is part of preprocessing the data.


To make the data of ‘CLOCK’ useful I had to convert given data into a meaningful type. It was of ‘object’ datatype which we converted to ‘datetime64’ type with the help of python.




## 7.3 Cleaning the Data



Cleaning of data is an important step in Data Analysis. If this is not done properly, it could hamper the ML models performance. This step includes deep analysis of each column and note down their nature.

In this project we saw many data columns to be skewed. Using seaborn library, we looked at all the data columns at once. We saw many outliers in many of the data columns given to us. Some were of that nature itself. Some of the data given to us was skewed by nature and I had to use that data into the ML model I was using. We replaced all the outliers present in many of the parameters with their respective averages. This helped make our data more evenly distributed, but the data was still skewed. Using pandas library, we used logarithmic codes to multiply our skewed data and make them more better for our Data Analysis.

  
before

  
after

I had to do some research on Feature Creation as it was new to me. In this, we have to create a feature which could take the place of a few columns of data. By visualising the data using correlation heatmaps, we found many significantly similar columns and a few columns which were unrelated to any other column. All those were merged into one column and the unrelated columns were deleted from the data provided.

  
before  
  
  
after

## 7.4 Data Modelling

We have many data models to try. We can’t always tell which model will suite the best for a given data. By understanding the data, we know that this data can only be analysed using regression models. We used 14 different Regression models to check which will give the best result. Eliminating the least scored and the overfit models, we found a few which were suited for our given dataset.


## 7.5 Model Optimization

Only using basic Machine Learning models will only take you so far. We have to optimize the models we have used. We have a few ways to do that. I used 3 techniques to further improve the results of our top models. We used GridSearchCV, RandomizedSearchCV and k-fold validation for this analysis. Improving the results of our models is very helpful as it can greatly affect the outcome of our analysis.

# Selection of Machine Learning Tools


## 8.1 Linear Regression

Linear Regression is a foundational statistical technique used in Data Analysis to model the relationship between a dependent variable and one or more independent variables. The model calculates the best-fitting line by minimizing the sum of squared differences between predicted and actual values, providing insights into patterns and trends within the data.



## 8.2 Random Forest Regression

Random Forest Regression is an ensemble learning method that combines multiple decision trees to predict continuous outcomes. It constructs numerous tree structures and aggregates their predictions to reduce overfitting, enhancing accuracy and robustness in analyzing complex datasets.



## 8.3 Support Vector Regression (SVR)

It employs support vector machines to find a hyperplane that best represents the relationship between variables while minimizing error. SVR aims to fit a function within a specified margin of error around the predicted values, allowing for flexibility in handling non-linear relationships between features and the target variable.

## 8.4 Ridge Regression

Ridge Regression is a technique that adds a penalty term to the ordinary least squares method, aiming to shrink the coefficients toward zero. The added penalty term, controlled by a hyperparameter (alpha), trades off between fitting the data well and keeping the coefficients small, making it particularly useful in handling multicollinearity in predictive modeling tasks.

## 8.5 Lasso Regression


Lasso Regression is a technique that incorporates L1 regularization. It introduces sparsity by encouraging some coefficients to be exactly zero, effectively performing feature selection. This method helps in creating simpler models by automatically identifying and excluding less influential predictors, enhancing interpretability and reducing model complexity.

## 8.6 Least Angle Regression (LARS)

LARS (Least Angle Regression) is a regression technique used in data analysis and machine learning for variable selection and model building. It sequentially adds predictors while controlling the coefficients' growth by moving in the direction most correlated with the response variable. LARS is particularly adept at handling situations with a high number of predictors, providing a path-based approach to feature selection and regularization, making it efficient and suitable for high-dimensional datasets.


## 8.7 Gradient Boosting

Gradient Boosting Regression is an ensemble learning technique that builds a predictive model by combining the output of multiple weak learners sequentially. It works by minimizing errors from previous models, creating new models that focus on the residual errors. This iterative process, using decision trees as base estimators, leads to a strong predictive model robust against overfitting, often offering high accuracy in predicting continuous target variables. The method is versatile, adaptable to various data types, and capable of handling complex relationships within the dataset.



## 8.8 XGBoost

XGBoost Regression is a powerful machine learning algorithm known for its exceptional predictive performance. It's an ensemble method that combines multiple decision trees to produce highly accurate regression models. Through gradient boosting, it optimizes model performance by minimizing prediction errors, making it a popular choice for various regression tasks in data analysis and predictive modeling.



## 8.9 Elastic Net Regression


Elastic Net Regression is a hybrid model combining Lasso and Ridge regression techniques, incorporating both L1 and L2 regularization penalties. This method is effective in handling datasets with a large number of features, providing a flexible approach to regression tasks by controlling the trade-off between bias and variance.

## 8.10 Bayesian Ridge Regression

Bayesian Ridge Regression is a statistical model that combines Bayesian methods with linear regression. It assumes a prior distribution over regression coefficients, allowing for uncertainty estimation in predictions. This technique automatically determines the regularization parameters.

## 8.11 Kernel Ridge Regression

Kernel Ridge Regression (KRR) is a non-parametric regression technique that combines Ridge Regression with kernel methods. KRR uses a kernel function to compute similarity between data points, allowing it to capture complex patterns in the data while controlling overfitting through regularization via the ridge penalty term. Its flexibility makes it suitable for handling non-linear and noisy data in regression tasks.




## 8.12 Stochastic Gradient Descent (SGD)

It optimizes the regression coefficients iteratively by minimizing the difference between predicted and actual values, gradually adjusting the weights based on individual samples. SGD efficiently handles large datasets due to its stochastic nature, updating parameters using small, random subsets of data at each iteration, making it suitable for real-time and online learning scenarios.

## 8.13 Decision Tree Regression

Decision Tree Regression is a non-linear regression algorithm that partitions data into segments, predicting continuous values by averaging the target variable within each segment. This model is versatile, handling complex relationships between variables and offering interpretability at the cost of potential overfitting with deep trees.



## 8.14 adaboost Regression

AdaBoost Regression is an ensemble learning technique that combines multiple weak learners, typically decision trees, to create a robust predictive model. It sequentially adjusts weights on n-correctly predicted instances, emphasizing their significance in subsequent models.

## 8.15 Table showing the differential characteristics of each model

|  |  |  |
| --- | --- | --- |
| Number | ML Model | Differential Characteristic |
| 1 | Linear | Simple model for linear relationships. Susceptible to overfitting. |
| 2 | Random Forest | Ensemble of decision trees, often robust to overfitting and outliers. Good for non-linear relationships. |
| 3 | SVR | Support Vector Machine for regression, handles non-linear relationships using kernels. Effective for high-dimensional data. |
| 4 | Ridge | Regularizes linear regression to prevent overfitting, shrinks coefficients towards zero. |
| 5 | Lasso | Regularizes linear regression, can also perform feature selection by setting some coefficients to zero. |
| 6 | LARS | Efficient algorithm for fitting linear models with L1-regularization (Lasso) or L2-regularization (Ridge). |
| 7 | Gradient Boosting | Sequentially builds trees, each correcting errors of previous trees. Prone to overfitting without careful tuning. |
| 8 | XGBoost | Highly optimized implementation of gradient boosting, efficient and scalable. |
| 9 | Elastic Net | Combines L1 and L2 regularization for flexibility in handling feature selection and preventing overfitting. |
| 10 | Bayesian Ridge | Bayesian approach to linear regression with L2-regularization, incorporates uncertainty in estimates. |
| 11 | Kernel Ridge | Extends linear regression to non-linear relationships using kernels. |
| 12 | SGD | Stochastic gradient descent, efficient optimization for large-scale datasets, but sensitive to hyperparameters. |
| 13 | Decision Tree | Easily interpretable model that splits data based on decision rules. Prone to overfitting. |
| 14 | AdaBoost | Ensemble method that sequentially builds weak learners (often decision trees) and focuses on misclassified examples. |

# Best Suitable ML Tool

From the analysis done till this point, we have found XGBoost and and Gradient Boosting Regressor to give the best fruits of them all. They weren’t overfitting and also gave the best result from the others.

Doing model optimization is important for getting better and proper results. Sometimes, we don’t get the desired numbers on simply passing the data through our model. We have to tweak it a bit to make the model understand our data and make correct predictions in the future for the benefit of the industry.

I then made them go through some optimizations. Using GridSearchCV, RandomizedSearchCV and k-fold validation methods, we reached an acceptable score.

# Conclusion

* For the input data received, it is important to do visualization, preprocessing, remove the outlier and eradicate skewness of the data as far as possible before using machine learning tools for analysis.
* Data generated at Sinter plant could be analyzed by using 14 Machine Learning Models.
* XG Boost and Gradient Boosting Regressor gave the best results.
* These 2 ML models gave the accurate prediction for the given data fed.
* Best Value obtained was 79% using XG Boost with Randomized Search CV.

# References

* SK Learn website - <https://scikit-learn.org/stable/index.html>
* Tata Steel Iron Making and Steel making process report.
* Tata Steel Standard Operating Procedure (SOP) for Sinter Process
* Regression Analysis Project referral done on Auto ML by VIT Student

# Acknowledgment

I wish to thank Mr Nitish Kumar, Head Analyst of Tata Steel, who guided me in this project. Also, would like to thank Mr R Krishna who sponsored my project and gave necessary guidance. I would like to thank one of my colleague Mr Kartik for his valuable input.

I also would like to thank my Prof. Ms Manju G. who guided me during the Internship.

Prepared By

Krishna Deshpande, VIT Chennai

…………………………………………………………… End of Document ………………………………………………………